防 護衣各部份所用的材質

| 化學防護衣常用的高分子 |
| --- |
| 名稱 | 請參照Bytyl |
| Butyl (97% isobutylene/ 3% isoprene copolymer |  |
| Chlorobutyl(butyl rubber with chlorine atoms substituted randomly for hydrogens) | 請參照Polyethylene |
| Chlorinated polyethylene (polyethylene with 36-45% by weitht chlorine atoms substituted randomly for hydrogen atoms) |  |
| EVA/PE(blend of 14% ethylene/ vinyl acetate copolymer; 86% polyethylene |  |
| EVOH (ethylene/vinyl alcohol copolymer) |  |
| Fluorine/Chlorporene (Viton, chloroprene laminate) | 請參照Viton, Neoprene |
| FEP, fluorinated ethylene propylene Resin (Hexafluoropropylene/ tetrafuoroethylene copolymer |  |
| FEP/TFE (FEP; tetrafluoroethylene blend) |  |
| Natural rubber (isoprene) |  |

| NBR, Nitrile (random or alternating acrylonitrile/butadiene copolymer |  |
| --- | --- |
| Neoprene (chloroprene) |  |
| Neoprene/SBR (chloroprene; styrene-butadiene blend) | 請參照Neoprene; SBR |
| Neoprene/Natural (chloroprene; isoprene blend | 請參照neoprene; Natural rubber |
| Polyethylene (ethylene) PVA(vinyl alcohol) | 請參照PVC; NBR |
| PVC (vinyl chloride) PVC/Nitrile (blend) |  |
| Saran (85% vinylidene chloride/15% vinyl chlride copolymer |  |
| Saranex (laminate of polyethylene and saran) |  |
| SBR (25% styrene/75% butadiene random copolymer) |  |
| Silver shield, 4H (laminates of polyethylene and EVOH) |  |
| Viton (hexafluoropropylene/ vinylidene fluoride random copolymer |  |
| Vitrile (Viton; nitrile blend) | 請參照Viton; NBR 請參照Natural; Neoprene; NBR (carboxylated nitrile Has carboxyl groups at the End of the polymer chains |
| Troionic (natural; neoprene; Carboxylated nitrile blend |  |

| Urethane (condensation product of a polyisocyanate and a polyol) |  |
| --- | --- |
| 常用淋膜材質 |
| Cellulose or cotton (polysaccharide, or polyalcohol) |  |
| Disposaguard (cellulose reinforced with nylon, i.e., scrim reinforyced) | 請參照cellulose |
| Duraguard (non-woven Polypropylene fibers) |  |
| Fiberglass (fibers of glass, usually coated with silicon or silanes) | May be added to many Polymers (polyester, nylon, Polypropylene) |
| Gore-Tex (TFE; polyester or nomex laminate) |  |
| Nomex (aramid fiber, polyamide) |  |
| Nylon (polyamide, condensation product of diamine and dicarboxylic acid, e.q., nylon 66) |  |
| Polyester (condensation product of ethylene glycol and terepthalic acid), e.q., Dacron and Sontara | 請參照”Fce Shield Polymers” |
| Rayon (regenerated cellulose fiber) | 請參照polyethylene |
| Safequard (three layers of polypropylene) | 請參照polyethylene |
| Tyvek (non-woven polyethylene fibers) | 請參照polyethylene |

防護衣材質

國內目前市面上常見的防護衣材質有：

(1)杜邦的泰維克(Tyvek)

泰維克是一種紡粘烯烴(Spun bonded olefin)纖維，不易撕裂，且具極佳的微粒捕捉特性，因此可用於石棉作業、粉塵作業場所的作業人員，同時也可用於噴漆業及製造業的一般用途。標準泰維克材質的防護衣雖透氣性較好，但只適用於Level C的危害狀況使用。

(2)泰維克淋膜

以標準的泰維加上一層黃色PE膜，以阻擋蒸，並可防止一些化學品的侵滲。防嚄效果較標準泰維克佳。

(3)Tyvek覆上SARANEX 23P*膜

多層熱塑性的膜覆蓋在泰維克上，以防多氯聯苯等物質的危害。

(4)Encase，美國Abanda公司出品

此種材質的防護衣國內較少見，其材質是以P.P.覆上PE膜，以提供足夠的強度及防撕性，同時PE層可防止化學品滲侵，且可防水及微粒。

(5)Chemtuff ，美國Chemron出品

一種利用多層防磨性材質做成的材質，對化學及生物性危害物質具防禦作用。

(6)Responder

Responder的材質是由美國的Kappler Safety Group所發展出的多層膜及合成物質組成，氣密性佳，可做為Level A 及B危害的防護。

＊“SARANEX”為美國DOW化學公司出品。

(7)Barricade

Barricade是杜邦公司以多層合成膜加上強化纖維製成，可對許多化學品提供長時間及有效的防禦功能，可於危害物緊急應變的狀況使用。符合Level A 或B的防護需求。

(8)Chemrel

美國Chemron研製的Chemrel及Chemrel Max材質是一名極強吸收性物質的伸縮纖維，其防護效果可符合Level A 及B的要求。

(9)CPF系列

美國Kevlar公司所發展的防護材質，目前有CPF1、CPF2、CPF3、CPF4四種不同防護等級的防護衣。

(10)歐洲製品

歐洲的產品在國內有的主要是Trellchem、Drager及Auer產品，其使用材質和化學防護手套類似，是把數種材質結合一起，以提供使用者足夠的保護。此類產品價格一般較美製產品高，通氣性較差，但可配備氣冷或水冷管，另外其外表一但有部份破損，並可予以修補，這點是一些美製產品所無法提供的部份破損，並可予以修補，這點是一些美製產品所無法提供的。

(11)日本製品

日製防護衣多以進口美製材質(泰維克等)再加工，另外則為防護等級較低的化學防護衣。

3.防護衣材質功能測試

防護衣對化學品的破出時間及滲透率也是由ASTM-F739的方法判定，部份防護衣的測試資料列表３－３。此種測試結果也可藉由文獻及製造商的測試報告獲得。若無現成測試資料，則得用實驗來判知。

三、面罩材質

密閉性防護衣的另一重要注意部份是其面罩所用材質，面罩材質使用不當有可能影響到防護效果。一般常用來做面罩的材質及結構請參照表3-4。

表3-4　防護衣面罩所用材質

| Acetate (cellulose acetate, acetate ester of cellulose). | 請參照 cellulose |
| --- | --- |
| Acrylic (methylmethacrylate) |  |
| Cellulose propionate (propionic ester of cellulose) | 請參照 cellulose |
| CR-39 (diethylene glycol bis allylcarbonate) |  |
| Polycarbonate (condensation product of bisphenol-A and phosgene) |  |
| Polyester (condensation product of dicarboxilic acid and glycol; for example terepthtalic acid and ethylene glycol) |  |
| Poysulfone (condensation product of bis-phenol a and dichlorophenyl sulfone) |  |
| PVC (vinyl chloride) |  |
| Surlyn (ethylene/methacrylic acid, random copolymer |  |